SPECIFICATION

Section 07900

WaboCrete® Parking Series “Gray”

Elastomeric Concrete Header and Blockout Infill Material

PART 1 - GENERAL

1.01	Work Included

A.	The work shall consist of furnishing and installing elastomeric concrete headers and blockout infills in accordance with the details shown on the plans and the requirements of the specifications. In the event of any discrepancy between the contract drawings and specifications, the specifications shall govern.

B.	Related Work

- Cast-in-place concrete

- Concrete Repair

- Expansion Joints

- Waterproofing

1.02	Submittals

A.	Standard Product Data - Submit typical product data sheet. Approved installers shall prepare and submit details of all special conditions to the manufacturer for review and approval prior to installation.

1.03	Product Delivery, Storage and Handling

- Deliver products in each manufacturer's original, intact, labeled containers, pallets or bundles and store under shelter in a dry location with temperatures above 40°F until installed. Store off the ground, protect from freezing, direct sun exposure in elevated temperatures and construction activities.

1.04	Acceptable Manufacturers

A.	All products shall be manufactured/supplied by Sika Emseal, 25 Bridle Lane, Westborough, MA 01581 USA

B.	Alternate manufacturers and their products will be considered, provided they meet the design concept and are produced of materials that are equal to or superior to those called for in the base product specification.

- Any proposed alternate systems must be submitted and receive approval 21 days prior to the bid.  All post bid submissions will not be considered. This submission shall be in accordance with MATERIALS AND SUBSTITIONS.

- Any manufacturer wishing to submit for prior approval must provide the following:

- A sample of the proposed elastomeric concrete with a letter describing how the material is considered superior to the specified product.

- Any substitution products not adhering to all specification requirements within, will not be considered.

1.05	Quality Assurance

A.	Warranty: Standard material limited warranty or project specific warranty available.

B.	Manufacturer: Shall have a minimum ten (10) years experience specializing in     the design and manufacture of Architectural Expansion Control Systems.

C.        Application: Minimum 2 years [documented] experience in work of this Section.

##### PART 2 - PRODUCT

2.01 	General – components and materials.

A.    	Elastomeric Concrete Header:  (WaboCrete Parking Series)

Material shall be an ambient cure, 100% solids, two component polyurethane with pregraded aggregate mix exhibiting the physical properties listed in the tables below.  When properly mixed and poured, the elastomeric concrete cures rapidly, flows and fills any voids, spalls or irregularities forming a monolithic unit.

Base Color: Gray

1.  Elastomeric cured binder and aggregate shall meet the following physical properties:

PHYSICAL PROPERTIES      ASTM METHOD       REQUIREMENTS          TEST RESULTS

Compressive Strength             D695 Mod                    2200                             2723 psi

Resilience at 5% deflection      D695                             90 (min.)                         96.7%

Adhesion to concrete:              C190

Dry Bond                                                  400                              451.3 psi

Wet Bond                                                  250                             353.9 psi

Impact Resistance                  Steel ball drop (.375” th. Disc / dry steel plate)

At  -20 deg F(-29C)                                         no cracks at 5 ft                7.0 ft-lbs

At   32 deg F (0C)                                            no cracks at 5 ft              10.0 ft-lbs

At 158 deg F (70C)                                          no cracks at 5 ft              10.0 ft-lbs

B.	Bonding Agent

Provide manufacturer’s two component, 100 percent solids bonding agent and apply to the sides and base of the preformed blockouts prior to placement of WaboCrete® elastomeric header. Store, mix and apply in accordance with manufacturer’s system data sheet.

Liquid components shall be identified by the following information:

Part A - Resin; Color:  Clear

Part B - Activator; Color:  Tan

C.	Accessories - Provide necessary and related accessories including broadcast aggregate for a complete installation.

2.02		Packaging

A.	Elastomeric  Header - Activator packaged in one-half gallon containers (Part A), resin packaged in gallon containers (Part B), 60 pound containers of aggregate (Part C) and broadcast aggregate shipped on wooden pallets, shrink wrapped.

2.03    Color and Finishes

Elastomeric Header base material shall be supplied in standard color: Gray.

Elastomeric Header material after field application of broadcast aggregate granules:  Gray-textured.

PART 3 - EXECUTION

3.01	INSTALLATION

A.	Preparation of the Work Area

1.	The contractor shall provide a properly formed, solid concrete blockout per the manufacturer and project requirements. Any edge or area in need of repair shall utilize one of the Sika Emseala concrete repair materials to provide a solid and square blockout. Call Sika Emseal Technical Support Services at (508) 836-0280.

2.	The contractor shall clean the concrete blockout of all contaminants and impurities by sandblasting immediately prior to elastomeric concrete installation. Concrete form release agents, water repellents, laitance, surface dirt and rust, all old sealants and other surface treatments and protective coatings are examples of materials which must be removed from the blockout substrate surface in order to obtain proper elastomeric concrete bond.

3.	Areas adjacent to the work area must be masked with building paper and tape to assure neat, clean lines.

4.	The blockout area must be completely dry for the installation of the elastomeric concrete header. Concrete must be cured a minimum of 14 days.  Wabo®Bonding Agent must be applied to blockout just prior to placement of WaboCrete Parking Series. When the use of patching compounds is required for blockout repair, follow manufacturer’s guidelines for the recommended cure times prior to placement of WaboCrete Parking Series elastomeric concrete.

5.	The blockouts must be made to the dimensions and elevations shown on the standard system drawings. Deviations from these dimensions will not be allowed without the written consent of Sika Emseal.

6.	Mix all WaboCrete Parking Series components in strict accordance with most current manufacturer’s installation procedures. Installing contractor shall confirm that they are in possession of the latest procedures prior to beginning work. Refer to website for current information.

3.02	CLEAN AND PROTECT

Protect work areas using WaboCrete Parking Series elastomeric concrete during construction. Heavy vehicles will not be permitted to cross the area without specific and written permission by the Engineer. Sub sequential damage to the installation shall be repaired at the contractor’s expense.